[image: image1.jpg]-~
(e} AMDRECOR





HF-3 Headframe Foam and Adhesive
Material Information*

I. FOAM MATERIAL:

Cross-Linked Polyethylenes
	Material
	Density lbs./ft³
	Tensile Strength psi., min.
	Compression Set 50% Deflection
	Operating Temperature
	Flammability Rating

	2# X-link PE
	2
	49
	21%
	-110° - 200°
	Available UL-94 HF-1


II. ADHESIVE MATERIALS:

Rubber Based Pressure Sensitive Adhesives

Standard 60# polyethylene silicone treated release liner
Thickness 

Exposed Side Adhesive 1.4 mils 

Liner Side Adhesive 1.1 mils 

Peel Adhesion - PSTC #3, no dwell, backed with 1 mil polyester 

Exposed Side 7.0 - 9.0 lbs/inch width 

Liner Side 6.0 - 7.5 lbs/inch width 

Shears - PSTC #7 modified, no dwell, 1/2" X 1/2" X 1000 gm, @ 72°F 

Exposed Side 24 + hours 

Liner Side 24 + hours 

Tensile - 10 lbs/inch width 

Elongation - 70%

* Source: S&S Plastics, Inc. 310 Sherman Avenue Newark, NJ 07114
                Phone: 973.624.1116  Fax: 973.624.8470
Amdrecor, Inc. 

Phone 800-356-2938
7019 Breen Dr 

www.amdrecor.com


Houston, TX 77086

info@amdrecor.com

[image: image1.jpg]